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631  Synthetic Leather Printing Emulsion
Water-Based Printing Materials
PRODUCT DESCRIPTION
Designed for PU/PVC synthetic leather substrates with dedicated leather printing coatings. After high-temperature curing and surface sealing, the system provides moderate substrate flexibility, tensile resistance and reduced cracking, with strong integration between the printed layer and the leather substrate.
KEY CHARACTERISTICS
• Strong color fastness with water and stain resistance.
• Natural surface texture while retaining the original hand and texture.
• Supports solid colors, gradients and geometric patterns.
• Supports high-definition digital patterns and multiple printing effects.
• Suitable for embossed, smooth, matte and glossy synthetic leather substrates.
TECHNICAL PROPERTIES
	Appearance
	Milky white liquid

	Solid Content
	±22%

	pH
	7-9


RECOMMENDED USE
Suitable for luggage fabrics, automotive interiors, sofa upholstery, belts, stationery packaging and outdoor leisure products.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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631  合成革印花乳液
水性印花专用材料
产品描述
以PU/PVC合成革为基材，搭配专用皮革印花涂料，经高温固化，表面封底处理成型，基材柔韧度适中，抗拉伸，不易开裂，印花层与皮革基材深度结合。
主要特性
• 色彩牢固不褪色，防水，防污
• 表面纹路自然，保留原有手感与质感
• 可实现纯色，渐变，几何图案
• 高清数码图案，多种印花效果
• 适合压纹，平纹，哑光，亮面等各类合成革基材
技术参数
	外观
	乳白色液体

	固含量
	±22%

	pH值
	7-9


使用建议
适合于箱包面料，汽车内饰，沙发软包，皮带，文具包装，户外休闲用品等。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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