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H-97  Black Water-Based Pigment
Water-Based Pigments – H High-Performance Series
PRODUCT DESCRIPTION
H-Series High-Performance Water-Based Pigment
KEY CHARACTERISTICS
• High weather resistance.
• Excellent migration resistance.
• Excellent temperature and solvent resistance, with acid/alkali resistance.
• High color vividness and transparency.
• High pigment content and strong covering power.
• The source manual states “Zero VOC”; product-specific verification is required before external compliance use.
• The source manual states compliance with international environmental standards; product-specific documentation should be verified before external compliance use.
TECHNICAL PROPERTIES
	Color / Product Name
	Black

	Lightfastness – Full Shade
	8

	Lightfastness – With White
	7-8

	Migration Resistance – Against PVC
	5

	Solvent Resistance – Toluene
	5

	Solvent Resistance – Butyl Acetate
	5

	Pigment Type
	Inorganic Pigment


RECOMMENDED USE
For PU leather, microfiber leather, recycled leather coatings, automotive seating leather, export leather, and products requiring wet-flex and perspiration-resistance testing.
STORAGE & HANDLING
Mix thoroughly before use and reseal the container immediately after use to reduce drying/skin formation and deterioration at high temperature. When color matching, use as few single-color components as practical and select base colors close to the target shade. For black leather finishing that will undergo high-frequency processing, verify suitability by testing in advance.
SOURCE NOTE
The source manual includes broad environmental statements for the H series. They are reproduced with qualification and should not be treated as product-specific certification without supporting documentation.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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H-97  黑色水性色浆
水性色浆（H系列高物性）
产品描述
H-系列高物性水性色浆
主要特性
• 高耐侯性能
• 优异的耐迁移性
• 优异的耐温、耐溶剂性及耐酸碱性
• 高鲜艳性及高透明性
• 最高的颜料含量及最优的遮盖力
• 零VOC
• 符合国际环保标准
技术参数
	品名
	黑色

	耐光性（单色）
	8

	耐光性（配白）
	7-8

	耐吐移（对PVC）
	5

	耐溶剂（甲苯）
	5

	耐溶剂（正丁酯）
	5

	颜料类别
	无机颜料


使用建议
应用于PU革、超纤、再生革涂层、汽车座椅革、出口革、需要湿挠曲、耐汗液测试产品。
储存与使用
使用前必须充分搅拌均匀，使用后必须立即密封容器。防止高浓度的颜料干燥凝结在容器上，以及在高温季节产生腐败变质现象。 调色时需要使用尽可能少的单色，并应该使用尽可能与要求色调接近的基色来调色。 成品革需经高周波工艺的黑色皮革涂饰，请先试验其适用性。
来源说明
说明书对H系列同时记载“零VOC”和“符合国际环保标准”；公开合规使用前应结合具体产品证明文件复核。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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