FAST  富可耐   |   TECHNICAL DATA SHEET

H-97  Black Water-Based Pigment

Water-Based Pigments – H High-Performance Series

PRODUCT DESCRIPTION

H-Series High-Performance Water-Based Pigment

KEY CHARACTERISTICS

• High weather resistance.

• Excellent migration resistance.

• Excellent temperature and solvent resistance, with acid/alkali resistance.

• High color vividness and transparency.

• High pigment content and strong covering power.

• The source manual states “Zero VOC”; product-specific verification is required before external compliance use.

• The source manual states compliance with international environmental standards; product-specific documentation should be verified before external compliance use.

TECHNICAL PROPERTIES

| Color / Product Name | Black |
| --- | --- |
| Lightfastness – Full Shade | 8 |
| Lightfastness – With White | 7-8 |
| Migration Resistance – Against PVC | 5 |
| Solvent Resistance – Toluene | 5 |
| Solvent Resistance – Butyl Acetate | 5 |
| Pigment Type | Inorganic Pigment |

RECOMMENDED USE

For PU leather, microfiber leather, recycled leather coatings, automotive seating leather, export leather, and products requiring wet-flex and perspiration-resistance testing.

STORAGE & HANDLING

Mix thoroughly before use and reseal the container immediately after use to reduce drying/skin formation and deterioration at high temperature. When color matching, use as few single-color components as practical and select base colors close to the target shade. For black leather finishing that will undergo high-frequency processing, verify suitability by testing in advance.

SOURCE NOTE

The source manual includes broad environmental statements for the H series. They are reproduced with qualification and should not be treated as product-specific certification without supporting documentation.

Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.

FAST  富可耐   |   技术数据表

H-97  黑色水性色浆

水性色浆（H系列高物性）

产品描述

H-系列高物性水性色浆

主要特性

• 高耐侯性能

• 优异的耐迁移性

• 优异的耐温、耐溶剂性及耐酸碱性

• 高鲜艳性及高透明性

• 最高的颜料含量及最优的遮盖力

• 零VOC

• 符合国际环保标准

技术参数

| 品名 | 黑色 |
| --- | --- |
| 耐光性（单色） | 8 |
| 耐光性（配白） | 7-8 |
| 耐吐移（对PVC） | 5 |
| 耐溶剂（甲苯） | 5 |
| 耐溶剂（正丁酯） | 5 |
| 颜料类别 | 无机颜料 |

使用建议

应用于PU革、超纤、再生革涂层、汽车座椅革、出口革、需要湿挠曲、耐汗液测试产品。

储存与使用

使用前必须充分搅拌均匀，使用后必须立即密封容器。防止高浓度的颜料干燥凝结在容器上，以及在高温季节产生腐败变质现象。 调色时需要使用尽可能少的单色，并应该使用尽可能与要求色调接近的基色来调色。 成品革需经高周波工艺的黑色皮革涂饰，请先试验其适用性。

来源说明

说明书对H系列同时记载“零VOC”和“符合国际环保标准”；公开合规使用前应结合具体产品证明文件复核。

资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。