FAST  富可耐   |   TECHNICAL DATA SHEET
PU-329  Soft-Matte Surface Treatment Agent
Water-Based Surface Treatment Materials
PRODUCT DESCRIPTION
A water-based soft-matte surface-treatment emulsion.
KEY CHARACTERISTICS
• Provides a smooth appearance.
• Soft matte effect.
• Improves dry/wet rub resistance.
• Weather and flex resistance.
TECHNICAL PROPERTIES
	Appearance
	Milky white liquid

	Solid Content
	±20%

	pH
	6-8


RECOMMENDED USE
Mainly used on PU and PVC synthetic leather surface coatings, including automotive interiors, sofa leather and luggage leather. A crosslinker may be added to achieve higher physical performance.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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PU-329  雾光表处剂
水性表面处理材料
产品描述
是一种新型雾光水性表处剂乳液
主要特性
• 具有平滑的外观
• 柔软的雾光效果
• 提高耐干湿擦性
• 耐候性，耐曲挠性
技术参数
	外观
	乳白色液体

	固含量
	±20%

	pH值
	6-8


使用建议
主要用于合成革（PU和PVC）表面涂层。通过添加交联剂，以获取更高物性，汽车内饰，沙发革，箱包革等。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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