FAST  富可耐   |   TECHNICAL DATA SHEET
PW-531  Silky-Feel Additive
Water-Based Post-Treatment Additives
PRODUCT DESCRIPTION
A special water-based finishing surface-treatment agent that provides a silky, skin-like and comfortable hand feel, with strong tape resistance and improved coating abrasion resistance.
TECHNICAL PROPERTIES
	Appearance
	Milky white liquid

	Solid Content
	±28%

	pH
	6-8


RECOMMENDED USE
Suitable for surface finishing layers on leather, synthetic leather, microfiber and textile (PU/PVC) systems. Dosage should be adjusted according to the process.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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PW-531  丝滑手感助剂
水性后处理助剂
产品描述
本品是一支特殊型水性涂饰表处剂，具有丝滑感，并且手摸有肤感，舒适，耐胶带性能强，同时提高涂层耐磨性
技术参数
	外观
	乳白色液体

	固含量
	±28%

	pH值
	6-8


使用建议
适用于皮革，合成革，超纤，纺织（PU、PVC）表面涂饰层，根据工艺定量。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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