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RU-3240  Medium-Soft Aliphatic Polyurethane Resin
Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Good overall performance.
• Excellent cold and flex resistance.
• Excellent UV resistance.
• Uniform appearance with excellent covering power.
TECHNICAL PROPERTIES
	Appearance
	Semi-transparent liquid

	Solid Content
	±30%

	pH
	6-8

	Character
	Medium-soft


RECOMMENDED USE
Suitable for leather, PU synthetic leather and microfiber leather, helping improve coating extensibility and yellowing resistance.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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RU-3240  中软脂肪族聚氨酯树脂
水性聚氨酯树脂
产品描述
脂肪族聚氨酯分散液
主要特性
• 良好的综合性能
• 特优耐寒性、耐曲挠性
• 特优的耐紫外线照射性
• 外观均匀，特优遮盖性
技术参数
	外观
	半透明液体

	固含量
	±30%

	pH值
	6-8

	特性
	中软


使用建议
适合于各种皮革，合成革（PU）、超纤，具有增加涂饰延伸力，耐黄变性能。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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