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RU-3280  Polyurethane Resin
Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Excellent light and yellowing resistance.
• Very strong adhesion.
• Excellent dry/wet rub resistance and water resistance.
• Improves fullness and comfort of hand while providing high gloss.
TECHNICAL PROPERTIES
	Appearance
	Semi-transparent liquid

	Solid Content
	±30%

	pH
	7-9

	Character
	Hard


RECOMMENDED USE
Suitable for a wide range of leather, synthetic leather and microfiber materials (PU/PVC), including sofa leather, automotive interior seating and luggage, for improving performance in mid/base coating layers.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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RU-3280  聚氨酯树脂
水性聚氨酯树脂
产品描述
脂肪族聚氨酯分散液
主要特性
• 具有极佳耐光、耐黄变性
• 极强的附着力
• 优异的耐干湿擦及耐水性
• 增加手感丰满舒适，高光泽
技术参数
	外观
	半透明液体

	固含量
	±30%

	pH值
	7-9

	特性
	硬


使用建议
可以广泛地使用各类皮革，合成革，超纤（PU、PVC），适合于各类沙发革，汽车内饰座垫，箱包等中底涂层提高物性等。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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