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RU-3320  Medium-Soft Aliphatic Polyurethane Resin
Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Improves coating water and scratch resistance.
• Excellent UV and flex resistance.
• Forms a tough, elastic film with excellent extensibility.
• Excellent embossing and shape-setting performance.
• Good stability and leveling.
TECHNICAL PROPERTIES
	Appearance
	Transparent liquid

	Solid Content
	±30%

	pH
	6-8

	Character
	Medium-soft


RECOMMENDED USE
Suitable for base coating layers on various leather, garment and footwear-upper applications to improve overall physical performance.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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RU-3320  中软脂肪族聚氨酯树脂
水性聚氨酯树脂
产品描述
脂肪族聚氨酯分散乳液
主要特性
• 增进涂饰的耐水性和耐刮性
• 特优紫外线照射性，曲挠性
• 成膜坚韧有弹性，延伸力特强
• 压花定型性特佳
• 具有良好稳定性和流平性
技术参数
	外观
	透明液体

	固含量
	±30%

	pH值
	6-8

	特性
	中软


使用建议
可广泛地使用各类皮革、服装、鞋面底涂层中，以提升总体的物性。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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