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RU-3330  Aliphatic Polyurethane Resin
Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Improves coating abrasion and scratch resistance.
• Forms a tough, elastic and soft film with very high weather resistance.
• Excellent overall performance with low surface loading and a clear grain appearance.
TECHNICAL PROPERTIES
	Appearance
	Transparent liquid

	Solid Content
	±30%

	pH
	6-8

	Character
	Soft


RECOMMENDED USE
Suitable for automotive seating, sofa leather, synthetic leather, microfiber leather, textile printing/dyeing and water-based ink applications.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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RU-3330  脂肪族聚氨酯树脂
水性聚氨酯树脂
产品描述
脂肪族聚氨酯分散乳液
主要特性
• 增进涂饰的耐磨耗和耐刮性
• 成膜坚韧有弹性，柔软且有超高耐候性
• 优越综合性能，用于皮面上不过负载，粒面清澈
技术参数
	外观
	透明液体

	固含量
	±30%

	pH值
	6-8

	特性
	软


使用建议
适用于汽车坐垫、沙发革等，也可以针对合成革、超纤、纺织印染、水性油墨等，应用广泛。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。


FAST | fukenai@salesfastinter.com | WhatsApp +1 682 358 9060 | salesfastinter.com




