RU-3340
Waterborne Polyurethane Resin										

Characteristics:
Aliphatic polyurethane dispersion

Application Characteristics:
1. Excellent UV radiation resistance
2. Excellent cold resistance, flex resistance
3. Excellent flexural fatigue resistance
4. Uniform appearance, and excellent extensibility
5. Clear and transparent film formation, smooth surface

	Appearance
	Transparent liquid
	
	

	Solid Content
	±30%
	
	

	pH Value
	7-8
	
	

	Characteristics
	Soft
	
	

	Ionicity 
	Anionic
	
	


Product Characteristics:   

Application Recommendations:
Suitable for (leather, PU) sofa leather, footwear upper, luggage leather, and midsole coating.

Storage Method:
Store in sealed original packaging at 5°C ~ 40°C for at least one year. After each use, the packaging should be resealed. Once opened, the product should be used up as soon as possible. This product must be protected from freezing. Must be mixed thoroughly before use.
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