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RU-3360  Waterborne Polyurethane Resin
Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Excellent cold resistance.
• Excellent flex resistance and uniformity.
• Forms a clear film with good weather resistance.
TECHNICAL PROPERTIES
	Appearance
	Transparent liquid

	Solid Content
	±30%

	pH
	7-8

	Character
	Medium-hard

	Ionicity
	Anionic


RECOMMENDED USE
Suitable for mid/base coating layers on leather, PU/PVC sofa leather, synthetic leather, microfiber leather, footwear uppers and luggage leather.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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水性聚氨酯树脂
产品描述
脂肪族聚氨酯分散乳液
主要特性
• 特优的耐寒性
• 特优曲挠性、均匀性
• 成膜通透，耐候性好
技术参数
	外观
	透明液体

	固含量
	±30%

	pH值
	7-8

	特性
	中硬

	离子性
	阴离子


使用建议
适合于（皮革，PU，PVC）沙发革、合成革、超纤、鞋面革、箱包革，中底涂层。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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