RU-6720 (Top Coat)
Aliphatic Polyurethane Resin									

Characteristics:
Aliphatic polyurethane dispersion

[bookmark: _GoBack]Application Characteristics:
1. Soft hand feel
2. Good aging resistance
3. Scratch resistance, yellowing resistance
4. Abrasion resistance, hydrolysis resistance
  
 Product Characteristics:
	Appearance
	Transparent liquid

	Solid Content
	±30%

	pH Value 
	7-9

	Characteristics
	Soft





Application Recommendations:
Can be widely used in various leathers (synthetic leather PU/PVC) coatings, luggage, footwear upper, and sofa leather. Enhances the high physical properties of leather finishes.

Storage Method:
Store in sealed original packaging at 5°C ~ 40°C for at least one year. After each use, the packaging should be resealed. Once opened, the product should be used up as soon as possible. This product must be protected from freezing. Must be mixed thoroughly before use.
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