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RU-6740  Polyurethane Topcoat Resin
Polycarbonate / Topcoat Waterborne Polyurethane Resins
PRODUCT DESCRIPTION
Waterborne aliphatic polyurethane dispersion.
KEY CHARACTERISTICS
• Forms a medium-soft, glossy film with excellent yellowing resistance.
• Excellent leveling with a comfortable coating hand.
• Good dry/wet rub and abrasion resistance.
TECHNICAL PROPERTIES
	Appearance
	Transparent liquid

	Solid Content
	±35%

	pH
	7-9

	Character
	Medium-soft


RECOMMENDED USE
Widely used as a topcoat on leather, synthetic leather and microfiber leather, including automotive seating and sofa leather, to improve coating performance.
STORAGE & HANDLING
Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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RU-6740  聚氨酯树脂（顶层）
水性聚氨酯树脂（聚碳/顶层）
产品描述
水性脂肪族聚氨酯分散乳液
主要特性
• 成膜中软、光亮、耐黄变极佳
• 流平性极佳，涂层手感舒适
• 耐干湿擦，耐磨耗性能好
技术参数
	外观
	透明液体

	固含量
	±35%

	pH值
	7-9

	特性
	中软


使用建议
广泛使用各类皮革顶层，可用于合成革和超纤顶层。用于汽车座椅革，沙发革，增强涂层物性。
储存与使用
5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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