FAST  富可耐   |   TECHNICAL DATA SHEET

RU-6860  Matte Polyurethane Resin

Matte Waterborne Polyurethane Resins

PRODUCT DESCRIPTION

Aliphatic matte polyurethane dispersion.

KEY CHARACTERISTICS

• Excellent cold flex resistance.

• Abrasion and scratch resistance.

• Smooth appearance and soft hand.

TECHNICAL PROPERTIES

| Appearance | Milky white liquid |
| --- | --- |
| Solid Content | ±35% |
| pH | 7-9 |
| Character | Medium-hard |

RECOMMENDED USE

Suitable for a wide range of leather and synthetic/microfiber leather (PU/PVC), including automotive leather, furniture leather and luggage. A crosslinker may be added to improve physical performance.

STORAGE & HANDLING

Store at 5°C–40°C in sealed original packaging. The source manual states a shelf life of at least one year under these conditions. Reseal after each use, use opened material as soon as practical, protect from freezing, and mix thoroughly before use.

Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.

FAST  富可耐   |   技术数据表

RU-6860  哑光聚氨酯树脂

水性消光聚氨酯树脂

产品描述

脂肪族哑光聚氨酯分散乳液

主要特性

• 优异的耐冷曲挠性

• 耐磨抗刮性

• 平滑的外观，柔软手感

技术参数

| 外观 | 乳白色液体 |
| --- | --- |
| 固含量 | ±35% |
| pH值 | 7-9 |
| 特性 | 中硬 |

使用建议

可以广泛地使用各类皮革，合成革，超纤（PU、PVC）汽车革，家具革，箱包，加入交联剂可提高物理性能。

储存与使用

5℃～40℃，密封的原包装中至少可以保存一年，每次使用后，应重新将包装密封，一旦开启包装，应尽快将内装产品用完，本品必须防冻保存，使用前必须混合均匀。

资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。