FAST  富可耐   |   TECHNICAL DATA SHEET

Y-510  Light Blue Water-Based Dye

Y-Series High-Concentration Water-Based Dyes

PRODUCT DESCRIPTION

Y-Series High-Concentration Water-Based Dye

KEY CHARACTERISTICS

• Can be diluted with organic solvent and water.

• Good color migration resistance.

• Bright shades with good physical resistance and lightfastness.

• Excellent penetration and level-dyeing characteristics on leather.

• Easy to use with broad applicability and no special dilution solution required.

• Good acid and alkali resistance.

• The source manual states that all dyes meet its azo-test requirements and do not contain nonylphenol; product-specific verification is required before external compliance use.

TECHNICAL PROPERTIES

| Color | Light Blue |
| --- | --- |
| Water Resistance | 5 |
| Acid Resistance (Column 1) | 6 |
| Acid Resistance (Column 2) | 5 |
| Wash Resistance | 3 |
| Dry-Cleaning Resistance | 4 |
| Toluene Resistance | 3 |

RECOMMENDED USE

The source manual emphasizes leather penetration, level dyeing and broad applicability, but does not provide a single end-use application list for each shade.

STORAGE & HANDLING

The source manual does not provide separate storage conditions for the Y series. Confirm current handling and storage requirements with FAST technical documentation.

SOURCE NOTE

The source physical-property table contains two columns both labeled “Acid Resistance”; they are retained here as Acid Resistance (Column 1) and (Column 2).

Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.

FAST  富可耐   |   技术数据表

Y-510  浅蓝染料水

Y系列高浓度染料水

产品描述

Y系列高浓度染料水

主要特性

• 具有使用有机溶剂与水稀释之特性

• 有很好的颜色耐迁移性

• 色泽鲜艳、物理耐性佳、耐光性优良

• 有极佳之皮革渗透均染特性

• 容易操作及广泛实用性且不需特殊稀释溶液

• 品质优良耐酸碱性佳

• 所有染料偶氮检测符合要求，且不含壬基酚

技术参数

| 颜色 | 浅蓝 |
| --- | --- |
| 耐水性 | 5 |
| 耐酸性（列1） | 6 |
| 耐酸性（列2） | 5 |
| 耐水洗 | 3 |
| 耐干洗 | 4 |
| 耐甲苯 | 3 |

使用建议

原说明书强调皮革渗透均染特性及广泛适用性，未列出单一终端应用清单。

储存与使用

原说明书未单独列出Y系列储存条件；使用与储存要求请以FAST当前技术资料为准。

来源说明

原说明书物性表包含两个均标为“耐酸性”的栏位；本TDS按原表保留为“耐酸性（列1）/（列2）”。

资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。