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Y-515  Royal Blue Water-Based Dye
Y-Series High-Concentration Water-Based Dyes
PRODUCT DESCRIPTION
Y-Series High-Concentration Water-Based Dye
KEY CHARACTERISTICS
• Can be diluted with organic solvent and water.
• Good color migration resistance.
• Bright shades with good physical resistance and lightfastness.
• Excellent penetration and level-dyeing characteristics on leather.
• Easy to use with broad applicability and no special dilution solution required.
• Good acid and alkali resistance.
• The source manual states that all dyes meet its azo-test requirements and do not contain nonylphenol; product-specific verification is required before external compliance use.
TECHNICAL PROPERTIES
	Color
	Royal Blue

	Water Resistance
	5

	Acid Resistance (Column 1)
	6

	Acid Resistance (Column 2)
	5

	Wash Resistance
	3

	Dry-Cleaning Resistance
	4

	Toluene Resistance
	3


RECOMMENDED USE
The source manual emphasizes leather penetration, level dyeing and broad applicability, but does not provide a single end-use application list for each shade.
STORAGE & HANDLING
The source manual does not provide separate storage conditions for the Y series. Confirm current handling and storage requirements with FAST technical documentation.
SOURCE NOTE
The source physical-property table contains two columns both labeled “Acid Resistance”; they are retained here as Acid Resistance (Column 1) and (Column 2).
	Source basis: FAST Product Manual v6 supplied for this project. This sheet reproduces source-manual data for technical reference. No warranty is expressed or implied; verify current specification and test suitability before use.
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Y-515  宝蓝染料水
Y系列高浓度染料水
产品描述
Y系列高浓度染料水
主要特性
• 具有使用有机溶剂与水稀释之特性
• 有很好的颜色耐迁移性
• 色泽鲜艳、物理耐性佳、耐光性优良
• 有极佳之皮革渗透均染特性
• 容易操作及广泛实用性且不需特殊稀释溶液
• 品质优良耐酸碱性佳
• 所有染料偶氮检测符合要求，且不含壬基酚
技术参数
	颜色
	宝蓝

	耐水性
	5

	耐酸性（列1）
	6

	耐酸性（列2）
	5

	耐水洗
	3

	耐干洗
	4

	耐甲苯
	3


使用建议
原说明书强调皮革渗透均染特性及广泛适用性，未列出单一终端应用清单。
储存与使用
原说明书未单独列出Y系列储存条件；使用与储存要求请以FAST当前技术资料为准。
来源说明
原说明书物性表包含两个均标为“耐酸性”的栏位；本TDS按原表保留为“耐酸性（列1）/（列2）”。
	资料依据：本项目提供的 FAST《富可耐水性涂层材料 产品说明书》v6。本表按原说明书整理，仅供技术参考，不具任何保证性质；使用前请确认当前规格并预先试验其适用性。
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